## Slide 1: photoacoustic physical unclonable function for scalable and stretchable skin electronics

## Slide 2: Contents
Section 1
Section 2
Section 3
Section 4
Section 5
Section 6

## Slide 3: Fabrication Process
a
100°C
Si
CH3
CH3
HO
O
H
n
1% AgNW solution
1000 – 5000 rpm
UV exposure
500 rpm
AgNW solution coating
PDMS hydrophilization
100°C
AgNW network
100°C
PDMS capping
AgNW network formation
Delamination
PDMS substrate
PDMS curing
PDMS
Glass/Dextran

## Slide 4
10 μm
PDMS
AgNW
PDMS
500 μm
Top view
Cross-section view

## Slide 5: Spin coating cycle – PUF parameter
Uniformity | Uniqueness | Entropy
11.94 | 21.02 | 0.52
20.60 | 32.70 | 0.72
31.80 | 43.40 | 0.89
50.02 | 50.05 | 0.98
50.00 | 50.04 | 0.98
Spin X1
Spin X2
Spin X3
Spin X4
Spin X5

## Slide 6: 지표 설명
Chip a: 00110100
Chip b: 01110011
Hamming Distance: 4
Inter-HD: 4/8 = 50%
Chip a: 00110100
Uniformity: 3/8 = 37.5%
Chip a: 00001111
Chip b: 01010101
확률 분포가 얼마나 균일한가
10
최댓값: 50%
최댓값: 50%
최댓값: 1bit

## Slide 7
Sample
2 axis-
motor
PC
SMF
532 nm
Laser control
Motor control
Galvo control
PA signal
C
C
OL
GM
RUT
Amp
PM
Coating cycle (#)
1
2
3
4
5
Binary
PA

## Slide 8
PDMS
Only BC
PDMS
Only SC
PDMS
SC + BC
Only SC (10% Strain)
SC + BC (10% Strain)
Physical attack
Physical attack
Dense AgNW
Stretched AgNW
Blade coating
Coating direction
-----------
Substrate Temperature = 60°C

## Slide 9
(D) 0% strain (E) 8% strain and (F) 10% strain
AgNWs : Graphene
1 : 4
1 : 2
1 : 1
2 : 1
GFmax
57.3
29.6
24.6
14.3
GF = (ΔR/R0) /strain
Figure 5. (A) Relative resistance changes strain curves of strain sensors based on AgNWs/
graphene mixed particles with different graphene and AgNWs mass ratios.

## Slide 10: Application
Authorized state
Privacy-lock state
Unauthorized state
System decision workflow
PUF key
PUF key
PUF key
101101...
101101...
000110...
PUF 2
PUF 1
PUF 1
Func
#1
(PUF)
Func
#2
(resist)
Func #3
(bioinfo)
Resistance
Resistance
Resistance
R/R0 < threshold
R/R0 > threshold
R/R0 < threshold
Attack detection
No detection
No detection
Bioinformation
access
Bioinformation
blocked
Bioinformation
blocked
Concept image
(example)
c
d
e
PUF key
check
PUF match
PUF match
PUF mismatch
Resistance check
R/R0 < threshold
(normal)
(R/R0 > threshold
ttack)
Bioinformation
access
Bioinformation
blocked
Match
Mismatch
PUF authorization
(initial state)
save

## Slide 11: Before/After PDMS capping
After
Before

## Slide 12: Random 10 of PUF

## Slide 13
Mouse ear
Photoacoustic
microscopy
Blood vessels on mouse ear