## Slide 1
Basics of
Synaptic Transistor
경북대학교 MENLAB 2025000422 최민수
26.01.04 MENLAB MEETING

## Slide 2
Introduction
- Emerging Neuromorphic systems
- Architecture of the Synapse devices
- Materials of Photo-Synaptic Transistor
- Persistent-Photoconductivity (PPC)
2. Neuromorphic Hardware System
- Artificial Neuron
- Leaky Integrate-and-Fire (LIF) model
- Synaptic Plasticity
- Performance Indicators of an Artificial Synapse
Contents

## Slide 3
Introduction

## Slide 4
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
https://www.kairnews.com/news/438729
Emerging Neuromorphic systems
Neuromorphic systems, which conduct “in-memory” computing, simultaneously perform computations and data processing.
von Neumann bottleneck
+
Artificial Intelligence (AI)

## Slide 5
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Li, Yibo, et al. "Review of memristor devices in neuromorphic computing: materials sciences and device challenges." Journal of Physics D: Applied Physics 51.50 (2018): 503002.
Architecture of the Synapse devices
Memristor Array
Resistance variation
Analog multilevel + Nonvolatile
Two-terminal
Offline learning
Presynaptic Spike
Voltage pulse
Postsynaptic Spike
Voltage pulse
Output
Postsynaptic Current (PSC)
Thin Film Transistor
Conductance variation
Analog multilevel
+ Nonvolatile or Semivolatile
ex) Floating Gate, Ferroelectric, PPC
Three or more terminals
Online learning
Presynaptic Spike
 Light pulse
Postsynaptic Spike
 VGS pulse
Output
IDS (PSC)
Initial
Current

## Slide 6
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Materials of Photo-Synaptic Transistor
Silicon
High switching performance
Suitable for digital computing
ex) CMOS
2D materials
Immature stage
+ Poor uniformity
+ Low stability
Perovskite
Limited to solution process
+ Pb inclusion
+ Low stability
Amorphous Oxide Semiconductor (AOS)
 Mature stage (Commercialized as n-type channel TFT)
+ High electron mobility in the amorphous phase
+ Lower leakage current due to wide bandgap energy
+ Persistent-Photoconductivity (PPC) effect

## Slide 7
Adv. Mater. 2021, 33, 2006091
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Persistent-Photoconductivity (PPC)
(d) PPC effect
1. Photoionization of Deep Traps (VO ⟶ VO+ or VO2+)  Photoelectron emission & Lattice Relaxation
2. Very high activation energy for neutralization (VO+ or VO2+ ⟶ VO )  Hindered recombination
3. Maintaining high conductance ()  Increasing retention time  Long-Term Potentiation (LTP)
(e)
Photonic input
Photoionization of VO
Conductance variation
(f)
Applying +VGS pulse
Alleviation of PPC
Long-term depression (LTD)/Reset
IDS(0): Current at the onset of decay
β: Distribution of defects that control the decay process
τ: Relaxation time

## Slide 8
Moon, Seung Jae, et al. "Photo response of a-IGZO thin films as a function of annealing temperature." Journal of Information Display (2025): 1-11.
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
How to Increase PPC Duration
Applying -VGS pulse  Suppress recombination
Sputtering process under low O2  Increase VO
Post-annealing at high temperature  Increase VO

## Slide 9
2. Neuromorphic Hardware System

## Slide 10
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Artificial Neuron
1. Dendrites: Receive signals from presynaptic axons and transmit them to the cell body (soma)
2. Soma: Spike generation occurs when presynaptic inputs exceed a specific threshold
3. Axon: A long fiber that conducts signals generated in the soma to the postsynaptic dendrites
4. Synapse: A junction between neurons that modulates and retains synaptic weight
Membrane: An insulating layer enclosing the soma that acts as a capacitor
Membrane potential: The electric potential of the membrane, which varies in response to input signals
Resting potential: The baseline membrane potential (reset) without stimulation (Biological: -V / Artificial: 0 V)
Light
IDS (PSC)

## Slide 11
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Leaky Integrate-and-Fire (LIF) model
LIF model: First reported as the IF model, the LIF neuron became the basis for artificial neurons
1. Presynaptic inputs
2. Raise the membrane potential above threshold
4. Time-dependent decay of membrane potential due to ion diffusion
3. Fire an action potential (spike)
to the postsynaptic dendrites
5. Reset to resting potential

## Slide 12
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Synaptic Plasticity
Standards for synaptic plasticity modulation
: “External inputs”, “Temporal correlation between the input and output spikes”
Electronic
Photonic
Pressure
Temperature
Synaptic Plasticity
Memory retention time
Short-term plasticity
Short-term depression (STD)
Short-term potentiation (STP)
Long-term plasticity
Long-term
depression / potentiation (LTD/LTP)
Ex) PPD
Ex) PPF
Long-term
depression / potentiation (LTD/LTP)
Spike-rate-dependent plasticity
(SRDP)
Spike-timing-dependent plasticity (STDP)

## Slide 13
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Short-Term Plasticity
Short-term plasticity, lasting milliseconds to minutes, underlies temporal information decoding
Paired-pulsed facilitation (PPF): A1 < A2

Paired-pulsed depression (PPD): A1 > A2

The former is a rapidly decaying function, and the latter is a slowly decaying one. (τ1 < τ2)
c1, c2 = initial facilitation amplitude / τ1, τ2 = relaxation time
ms~ s
ms~ s
Q. 생물학적인 관점에서 PPF와 PPD는 어떻게 발현될까?
Ans. PPF: “연속으로 오면 중요한 것이므로, 더 크게 반응해라!” ex) 민감화(산에 혼자 있는데 풀숲 발자국 소리), 집중, 긴급 상황(공포 영화 감상), 단기 기억
PPD: “처음엔 강하게 반응하지만, 반복되면 무시한다.” ex) 적응(냄새 맡기), 피로, 에너지 절약, 노이즈 필터링
Decay
Presynaptic spike interval

## Slide 14
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Actual Experiment of PPF/PPD
Polarity of Δω (PPF or PPD) depends on “A1 - A2”
Magnitude of Δω is modulated by the “ΔtLight”
Presynaptic Spike
Ex) 1st light pulse
Variable Setup
Ex) ΔtLight
Read Voltage
Ex) VDS + VGS pulse
Presynaptic Spike
Ex) 2nd light pulse
Read Voltage
Ex) VDS + VGS pulse
PSC Measurement
Ex) A1
PSC Measurement
Ex) A2
PPF or PPD

## Slide 15
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Long-Term Plasticity
Q. 생물학적 관점에서, 신호의 빈도와 동시성에 의해 결정되는 SRDP를 왜 Long-term plasticity로 간주해야 할까?
Ans. 뇌는 “자주 반복되는 사건”에 대한 기억을 영구적으로 저장하려고 하기 때문
Presynaptic spikes frequency
Spike-rate-dependent plasticity
SRDP: Frequency (ƒ) and Coincidence () is the key
 Long-term potentiation (LTP)
: Presynaptic spike frequency (ƒ) > 20
 Long-term depression (LTD)
: Presynaptic spike frequency (ƒ) < 10

## Slide 16
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Actual Experiment of SRDP
LTP: At higher frequencies, PPC accumulates and the current increases rapidly
LTD: At lower frequencies, PPC discharges before it can accumulate, resulting in no change or a decrease
Presynaptic Spikes
Ex) Light pulse train
Variable Setup
Ex) ƒ, ΔtLight
Read Voltage
Ex) VDS + VGS pulse
LTP or LTD
Reset Voltage
Ex) High +VGS
PSC Measurement
Ex) IDS, final
Q. 메커니즘(초기 자극 + 후속 자극  전류 변화)을 고려하였을 때, STP와 SRDP는 거의 비슷하다. 그럼 PPF의 지속 시간이 늘어난 것이 LTP인가?
Ans. “Transition from STP to LTP”
STP는 2번의 펄스 이후 금방 reset되는 상태이고, LTP는 Light pulse가 반복되면 PPC가 누적되어 전류의 베이스라인 자체가 높아져 자연적으로 reset이 되지 않는 상태

## Slide 17
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Long-Term Plasticity
Presynaptic spikes frequency
Spike-timing-dependent plasticity
Asymmetric STDP: Causality is the key
 Long-term potentiation (LTP)
: Δtpost-pre > 0,
Presynaptic spike (Light)  Postsynaptic spike (VGS)
Long-term depression (LTD)
: Δtpost-pre < 0,
Postsynaptic spike (VGS)  Presynaptic spike (Light)
Symmetric STDP: Coincidence () is the key
 Long-term potentiation (LTP)
: Regardless of order, ≈ 0
 Long-term depression (LTD)
: Regardless of order, > 0
Q. 생물학적 관점에서, 신호의 순서에 의해 결정되는 Asymmetric STDP를 왜 Long-term plasticity로 간주해야 할까?
Ans. 뇌는 “원인과 결과가 시간적으로 연결되어 있을 때(인과 관계)”에 대한 기억을 영구적으로 저장하려고 하기 때문

## Slide 18
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Actual Experiment of STDP
Variable Setup
Ex) ƒ, Δtpost-pre
PSC Measurement
Ex) IDS, final
Read Voltage
Ex) VDS + VGS pulse
Presynaptic-Postsynaptic Spike Pairing
Ex) Light pulse train (Pre) + VGS pulse train (Post)
Asymmetric, Symmetric LTP or LTD
Reset Voltage
Ex) High +VGS
Δtpost-pre represents only the x‑axis, while the y‑axis (Δω) becomes STDP only when the pulse shape, amplitude, or device parameters are continuously tuned until the device responds as intended

## Slide 19
Campbell, Kristy A., Kolton T. Drake, and Elisa H. Barney Smith. "Pulse shape and timing dependence on the spike-timing dependent plasticity response of ion-conducting memristors as synapses." Frontiers in bioengineering and biotechnology 4 (2016): 97.
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Anti-Hebbian Phenomenon in Experiments
Δtpost-pre < 0
PPC generation by pre-spike
Reset
by post-spike
Conductance increase
LTP
Δtpost-pre > 0
PPC suppression
by post-spike
PPC generation by pre-spike
Conductance reduction
LTD
Anti-Hebbian
Anti-Hebbian
Q. Anti-Hebbian 현상으로 인해 시냅스 가중치가 의도대로 형성되지 않는 문제를 극복하는 방법은 무엇이 있을까?
Ans. Pulse shaping: + VGS 사각파 대신 양전압과 음전압이 섞인 사인파 or 삼각파 사용
ex) Δtpost-pre > 0 : 빛이 들어올 때 Post Spike의 앞부분(음전압 or 낮은 전압)과 Pairing  Hebbian Rule
ex) Δtpost-pre < 0 : 빛이 들어올 때 Post Spike의 뒷부분(높은 양전압)과 Pairing  Hebbian Rule

## Slide 20
ACS Appl. Electron. Mater. 2022, 4, 1427−1448
Performance Indicators of an Artificial Synapse
Linearity
Ideal case) When x=ƒ and y=ω=, the relationship is y=ax+b
Experiment) Nonlinear conductance induced by trapping or PPC effects
Symmetry: Different mechanisms of PPC‑driven LTP and recombination‑induced LTD hinder achieving ‘ω-symmetry’
Dynamic Range = =
Number of Conductance States ( Multilevel Operation)
Ideal case) An infinite number of conductance states exist between and
Experiment) Noise and instability prevent an infinite number of reliably distinguishable conductance states
Ex) Typically 32–~64 levels (5~–6 bits) suffice for deep learning
Stability & Reproducibility
: Whether the weights are retained during the retention period, and whether the device continues to output the same values
Easy processability & Uniformity
Ex) Large‑area arrays fabricated with low‑cost, low‑temperature processes